## Slide 1: Innerlayer Copper Balancing Phase 2
© HDP User Group International
Team Leader:
Facilitator:
Implementation
Asa Guest, IBM
Karl Sauter
May 22, 2025
Host: Japan Pure Chemical

## Slide 2: Background
Localized areas of Innerlayer Copper Imbalance can result in localized innerlayer core deformation.
  Increasing Zo variation across high-speed channels
  Increases risk of Lamination voids, micro fracturing under large components
  Increased warpage & non-linear scaling
  Increases uncertainty/variation of layer z-axis location:
    Increasing backdrill stub variation
    Increased surface topology variations
Extent of Core deformation & Sensitivity to Inner Layer Copper Imbalance is an interaction between material selection and stackup.
Project Phase 1: Quantified sensitivity of void size and density stacking on core deformation, Surface topography for assembly, and recommended design approaches focused on Low Loss and Ultra Low-Loss laminates.
05/22/2025

## Slide 3: Phase 2 Motivation: Core Deformation and Insufficient Resin Fill
5/22/2025

## Slide 4: Phase 2 Motivation : Stackup and Material Selection
5/22/2025
Preventing core deformation requires filling voids on adjacent layers at same rate
When copper void volume is different between adjacent layers  prepreg thickness needs to be selected so that void fill rates are similar (most prominent with change in copper thickness)
Minimal deformation with either lower or higher flow when prepreg thickness match void volume ratio
Higher flow materials
Lower flow materials
High deformation with high flow
High deformation with low flow
Post Lamination

## Slide 5: Project Deliverables Phase 2
5/22/2025
5
CAD translator utility, a 3D translation rotation best fit (TRBF) algorithm, that will provide analysis of local copper distribution to identify risk areas for:
  Core deformation and backdrill stub variation (coplanarity)
  Surface topography variations
  Local areas of glass stop
Additional validation of model for mitigation of using different process flows (sub lam sequence and stack-up changes).
  Phase 1 was a "hammer test" with respect to design
  Quantify extent that construction stack-up can overcome unbalanced designs

## Slide 6: Member Benefits
5/22/2025
OEM & Designers: Improve copper fill design guidelines;
  Minimize impedance variations not captured in Zo coupons
  Minimize backdrill stub length variations under large BGAs
  Mitigate core deformation and surface deformation from copper distributions, also surface deformation and dynamic warpage
  Understand how laminate material properties can affect the design analysis for local copper balancing mitigating core deformation
  Reduce design costs and time to achieve more consistent electrical and topographical performance
ODMs: Understand the impact of copper distributions on dynamic warpage and boot issues (impedance variations, backdrill stubs)

## Slide 7: Member Benefits - Continued
PCB Fabricators: Identify potential risk areas for designers and understand to what extent resin material flow properties can modulate core deformation issues due to copper distributions.
Laminate Suppliers: Understand how resin flow properties, copper distributions, and stack-up parameters can impact core deformation.
Additional validation of the coplanarity and core deformation mitigation for sub lam sequence and stackup optimization. This will assure copper fill design rules are correct.
05/22/2025

## Slide 8: Phase 2 Model Assumptions/Disclaimers
Blurring algorithms are used as rough approximations to capture Cu density
Current algorithm assumes uniform ‘resin’ flow (kernel size is constant)
Meant to supplement other methods
  DFX
  Manufacturing experience
  Etc.

## Slide 9: Phase 2 CAD Translator

## Slide 10: Phase 2 Plan
Laminate Layers 9-14
  1-8 and 15-21
Goal 1 – Verify process alternative process steps improve coplanarity
  Quantify the difference
Goal 2 – Qualitatively analyze build data and simulation data for tool verification of risk areas
  Match Color Gradients to coplanarity/risk regions
  Rolling Average pixel count -> laminate material
    Need a TRBF algorithm to do analysis quantitatively
Supplier | Laminate Preferred | Contact
GCE (Site Undetermined) |  | Joe Beers
Victory Giant |  | Dana Korf
ACCL |  | Penny Lien
WUS |  | Greg Link
SCC |  | Sean Shi
TTM-DMC? |  | Todd/Ashley (Tent.)
TTM-FG? |  | Todd/Ashley (Tent.) John Konrad

## Slide 11: Phase 2 Plan, Cont.
PCB Fabricators
Material Selection
Test Vehicle Build Plan
Fabrication Notes
DFM

## Slide 12: Phase 2 Plan, Cont.
Laminate inner 2 oz cores (take coplanarity measurements)
Laminate 1 oz cores
Minimum of two lots (process to panel plate)
Segment panel into 4 quadrants and route x-section areas

## Slide 13: Phase 2 Analysis
Develop TRBF Algorithm to compare modeled to measured data
Measure Flatness across 4 quadrants using phase 1 params
  Compare results with phase 1 matching laminate types
X-Section same areas as Phase 1 analysis
  Thickness measurements
  Void analyses

## Slide 14: Phase 2 Analysis
Propose to use Single Value Decomposition
  Algorithm is complete for point clouds of the same size
  Need to develop algorithm to match different sized arrays
R² per axis: X=0.9998, Y=0.9998
Mean RMSE: 0.6127

## Slide 15: Process Flow
L2
L3
L(N-1)
5280x5280
2000x2000
2000x2000

## Slide 16: Thieving Updates
For non-manufacturing gerber data, the option to add thieving to the exterior of the panel must be available
Exploring different methods to add patterns that match the kernel size

## Slide 17: Status: Stackup Modulation; On Hold Until initial modeling of core deformation is more complete
5/22/2025
Use same TV from Phase 1 (22 layers, w/ six 2-oz layers)
Ensure any builds use same laminate / PCB fabricator combinations
  Build A: Increase prepreg thickness next to 2-oz layers by 100-150%
    Change the resin volume to match or exceed fill rate of adjacent 1-oz layers
    Goal to minimize or even flip direction of core deformation toward center
  Build option B: Fabricate the center 2-oz layers as sublam to decouple 1-oz vs 2-oz deformation.
Build option C: Hybrid construction using higher flow materials at center 2-oz
Analysis of surface topography and core deformation same as Phase 1
Builds only require fabrication through panel plate

## Slide 18: Project Flow Chart -
Fabrication
Evaluation
X-Section – Core Deformation measurements (1-2 panels/mtrl)
Design
(Cmplt)
Supplier 1 | Lower Flow Ultra Low Loss Laminate system Thick Prepreg @ 2oz lyrs 5 panels
Supplier 2 | 
Surface Topography (all panel/mtrl)
Data Analysis
Final Report
Supplier A | Lower Flow Ultra Low Loss Laminate system Hybrid 5 panels
Supplier B | 
Supplier C | Lower Flow Ultra Low Loss Laminate system Phase1 stackup w/ sublam 5 panels
Supplier D | 
Artwork Dev
Manual Testing
/ Verification
Deployment
Stackup Modulation of Core Deformation
Analysis Tool Dev
Interface Dev
Github Link
Complete

## Slide 19: Resources and Schedule
Task | Resource | Planned | Actual
Complete DOE Matrix | All |  | Complete
TV Design ECAD | Intel |  | Complete
PCB Laminate Materials | EMC, Iteq, AGC, TUC | 2025 July | 
TV Fabrication | TTM, WUS, VGT, SCC, Founder, SME, ACCL | 2025 September | 
Surface Characterization | Akrometrix | TBD | 
Microsection Analysis | Intel | 2025 November | 
Final Report | All | 2026 May | 
MetAve software dev | Artwork Conversion Inc |  | Complete
MetAve Testing / analysis | IBM | 2025 May | 
Wrapper Dev | IBM |  | Complete

## Slide 20: Team List
IBM - leader
AGC
Akrometrix
Panasonic
Oracle
Nokia
Juniper
WUS
Resonac
VGT
TTM
EMC
ITEQ
TUC
Co-Tech Development
Sanmina
Intel

## Slide 21
Thank You
For questions or comments on this presentation,
please email: karls@hdpug.org

## Slide 22: Appendix: Algorithm Information

## Slide 23: MetAve algorithm (Box Filter)
Command line executable
  Image operations become a file management issue
  Time Complexity:
  Assumes boundaries are 0
Inputs
  Input Layers
  Layer Weighting
  Averaging window
Weighted Result
Rolling average of target
N
N
Ncell(x, y)
r = 2

## Slide 24: Gaussian Algorithm
Accessed through the Scipy (pythons scientific computing library)
Time Complexity:
Adjustable parameters
  Etc.
May approximate physics closer than box blur

## Slide 25: Additional Algorithms To be Added
Median Filter
  May require multiple passes
Bilateral Filter
  Like Gaussian near strictly copper or strictly ‘prepreg’ regions
Open to adding others

## Slide 26: Appendix: Interface Information

## Slide 27: Interface Updates
Develop Interface for users to input stack up information/Gerber data
  Assign Layer Details (Cu Weight, core/PP thickness)
Pixel size is user defined
Additional Averaging algorithms
Additional Image Options
  Pan/Zoom/Rotate
  Colorization (User Color Schemes Added)

## Slide 28: Interface Updates, Cont.
Gerber to Tiff In App
In App Image View
Operations for stack up information from Gerber layers
Preset/User defined color mappings

## Slide 29: Interface Updates, Cont.
Layer specific modifications
Sub lamination Analysis
Additional user defined settings

## Slide 30: Interface Updates, Cont.
Sub lamination Analysis

## Slide 31: Appendix: Previous Copper Balancing Analysis
650um
0um
API utility from “Artwork Conversion Software, Inc.”
  Provide rolling grey scale average over a specified sliding window and window stepping;
    Allowing specific layer analysis w.r.t flow distances/properties of resin
    Ability to predict where deformation will start, locations of min/max deformation
  Provide ability to Add/Subtract multiple grey scale layers using layer weighting
Initial Wrapper created
to utilize API utility and
visualize results
Pixel size: 5x5mil
Total Copper
Visualization of 20% added thieving on signal layers

## Slide 32: Appendix: Previous Copper Balancing Analysis, Cont.
Example of Rolling Average over different distances
Pixel size at 5x5 mil
0.5 inch
1.25 inch
2.5 inch
Rolling average much better then simple averaging within a set grid w.r.t maintaining a level of local detail otherwise hidden.
Asymmetry of average thickness
Color bands around panel average

## Slide 33: Appendix: Previous Copper Balancing Analysis, Cont.
Panel 1, Mtrl A
Measured coplanarity variation of Q2
Shadow Moire
Total copper map of Q2 with rolling average
General patterns hold
Basic Shape of High/low areas
Location of Low/High Areas
Except when they don’t:
Panel 2, Mtrl A
Panel 1, Mtrl B
650um
0um

## Slide 34: Appendix: Previous Copper Balancing Analysis, Cont.
Measured coplanarity variation of Q4
Shadow Moire
Total copper map of Q4 with rolling average
General patterns hold
Basic Shape of High/low areas
Location of Low/High Areas
Panel 2, Mtrl A
Panel 1, Mtrl C
Total copper map as an indicator of coplanarity will be best when the local thickness variations are the dominate factor affecting coplanarity.
650um
0um

## Slide 35: Appendix: Previous Copper Balancing Analysis, Cont.
Changing color threshold mute or accent patterns and gradient detail;
White bands good for mapping areas to address with design
Full bands (jet, nipy_spectral) appear to have better visual correlation with Shadow-Moire measurements
650um
0um

## Slide 36: Backup

## Slide 37: Background (Phase 1) - Additional
5/22/2025
Stackup-up (prepreg selection matters for thickness control):
For same material prepreg thickness mattered

## Slide 38: Background (Phase 1) – Additional, Cont.
5/22/2025
Supplier | Material A | Material B | Contacts
SME | EM-890K | EM-528 | Brian Drummond, Alex Shen
VGT | EM-890K | EM-528 | George Dudnikov
ACCL | EM-890K | EM-528 | Vincent Yang
TTM | M-8000 | N4000-13EP | Ed Cullens, David Natz
WUS | IT-988GSE | TU-883 | Greg Link
SCC | IT-988GSE | IT-170GT | Vincent Wang
Founder | IT-988GSE | IT-170GT | 

## Slide 39: Asymmetry from Symmetric Design & Stackup
Asymmetric location of resin flow and core deformation likely critical to panel-panel variations in coplanarity and backdrill layer location.
Hypothesized to be related to book placement. But, outside of scope/focus of Phase 2
Why more resin here?
Stackup is symmetrical
5/22/2025